Product Name:  Colour Series ZT3481

Appearance:   A bright pink color, free flowing powder with a bright pearl luster

Ingredients and Composition

Chemical Name               %                CAS No.              CI No.

Mica                    49-52               12001-26-2              77019

Titanium Oxide(TiO2)            48-51               13463-67-7              77891

Direct Yellow 27               <1                10190-68-8              13950

Direct Red 80                <1                2610-10-8               35780

D50

Particle Size Distribution: 80% within the range 10-60 µm.       (By Malvern Mastersizer2000)

22.0±2.0

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       15-40 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)