Product Name: Exterior Fine Granary 96201WR

Appearance: A white, free flowing powder with a bland gold reflection color.

Ingredients and Composition

Chemical Name              %               CAS No.               CI No.

Synthetic Fluorphlogopite          42-46             12003-38-2

Titanium Oxide(TiO2)            52-56             13463-67-7               77891

Tin Oxide (SnO2)                  <1               18282-10-5               77861

Cerium Oxide (Ce2O3)                <1               1345-13-7                77280

Polymer                    1-5

D50

Particle Size Distribution: 90% within the range5-30µm.         (By Malvern Mastersizer2000)

14.5±1.5

Visual and Colorimetric evaluation:    conforms                    KCPP

pH (10% Aqueous Suspension):	           4.0 -9.0                    ISO787-9

Loss on Drying(105℃):	0.5 % max.                 GB 5211.3-85

Oil Absorption:                     60-90 g oil/100g powder        GB 5211.15-88

Bulk Density:                       20-45 g/100cm3              GB/T 23771-2009

Density                            2.8-3.4 g / cm3 (water=1)