SPECIFICATION

Cosray Rayspark Sparkling Red
(Code:SP8822)

INCI Name:                                Glass, Titanium Dioxide, Tin Oxide

Chemical Composition:	Test method

Glass	83.0-94.0%	CLRTM-51

TiO2	6.0-16.0%	CLRTM -48

SnO2	≤1.0%	CLRTM -48

Appearance:	Interference Red	CLRTM 52

Odor:	Odorless	CLRTM -52

Particle Size:	100-1500μm	CLRTM -42

pH-Value(10% Aqueous Suspension):	4.0-11.0	CLRTM -45

Oil Absorption:	40.0-75.0g/100g	CLRTM -46

Density	2.4-2.9g/cm3	CLRTM -47

Microbiology:		<100 cfu/g                                               CLRTM -54 No gram negative

Heavy Metals:	CLRTM -55

As	<3ppm

Pb	<10ppm

Hg	<1ppm

Sb	<2ppm

Cd	<1ppm

Zhongshan Zhongtai Pigment Co.,Ltd

Website: http://www.zsztyl.com	E-mail: zhongtaiyanliao@163.com